PROSOCO, Inc. Distributed by ZeroDocs.com

SECTION 07 19 00 – WATER REPELLENTS

 GENERAL

 SUBMITTALS

 Action Submittals:

 Product Data: Manufacturer’s descriptive data and product attributes.

 Closeout Submittals:

 Maintenance Data.

 QUALITY ASSURANCE

 Applicator Qualifications: Firm specializing in work of this Section, with minimum [2] [\_\_] years’ experience.

 Mockup: Minimum [\_\_x \_\_] feet.

 PRODUCTS

 MANUFACTURERS

 Contract Documents are based on products by PROSOCO, Inc. [www.PROSOCO.com](http://www.prosoco.com)

 Substitutions: [Refer to Division 01.] [Not permitted.]

 MATERIALS

 Water Repellent Coating:

 Product: Sure Klean Weather Seal Siloxane PD.

 Description: Water based, silane/siloxane water repellent coating.

 Solids content: 4 percent.

* + - 1. VOC content: Maximum 30 grams per liter.

\*\*\*\* OR \*\*\*\*

 Water Repellent Coating:

 Product: Sure Klean Weather Seal Siloxane WB Concentrate.

 Description: Water based, solvent-free silane/oligomeric alkoxysiloxane water repellent coating.

 Solids content: 48 percent.

* + - 1. VOC content: Maximum 41 grams per liter.

\*\*\*\* OR \*\*\*\*

 Water Repellent Coating:

 Product: Saltguard.

 Description: Solvent based, silane/siloxane water repellent coating and chloride screen.

 Solids content: 9 percent.

 VOC content: Maximum 713 grams per liter.

\*\*\*\* OR \*\*\*\*

 Water Repellent Coating:

 Product: Saltguard WB.

 Description: Water based, silane/siloxane water repellent coating and chloride screen.

 Solids content: 4.2 percent.

 VOC content: Maximum 25 grams per liter.

\*\*\*\* OR \*\*\*\*

 Water Repellent Coating:

 Product: Saltguard VOC.

 Description: VOC compliant, silane/siloxane water repellent coating and chloride screen.

 Solids content: 9.21 percent.

 VOC content: Maximum 100 grams per liter.

\*\*\*\* OR \*\*\*\*

 Water Repellent Coating:

 Product: Sure Klean Weather Seal Natural Stone Treatment.

 Description: Modified siloxane water repellent coating.

 Solids content: 9 percent.

 VOC content: Maximum 713 grams per liter.

\*\*\*\* OR \*\*\*\*

 Water Repellent Coating:

 Product: Sure Klean Weather Seal Natural Stone Treatment WB Plus.

 Description: Water based modified siloxane water repellent coating.

 Solids content: 15 percent.

 VOC content: Maximum 100 grams per liter.

\*\*\*\* OR \*\*\*\*

 Water Repellent Coating:

 Product: Sure Klean Weather Seal Natural Stone Treatment VOC.

 Description: Modified siloxane water repellent coating.

 Solids content: 9 percent.

 VOC content: Maximum 120 grams per liter.

 EXECUTION

 APPLICATION

 Apply in accordance with manufacturer's instructions.

 SCHEDULE

 Apply coatings to following exterior surfaces:

* + - 1. [Cast-in-place concrete.]
			2. [Precast concrete.]
			3. [Brick unit masonry.]
			4. [Concrete unit masonry.]
			5. [Stone.]
			6. [Cast stone.]
			7. [Brick] [Precast concrete] Stone] pavers.
			8. [\_\_\_\_.]

END OF SECTION