PROSOCO, Inc. Distributed by ZeroDocs.com

SECTION 07 19 00 – WATER REPELLENTS

GENERAL

SUBMITTALS

Action Submittals:

Product Data: Manufacturer’s descriptive data and product attributes.

Closeout Submittals:

Maintenance Data.

QUALITY ASSURANCE

Applicator Qualifications: Firm specializing in work of this Section, with minimum [2] [\_\_] years’ experience.

Mockup: Minimum [\_\_x \_\_] feet.

PRODUCTS

MANUFACTURERS

Contract Documents are based on products by PROSOCO, Inc. [www.PROSOCO.com](http://www.prosoco.com)

Substitutions: [Refer to Division 01.] [Not permitted.]

MATERIALS

Water Repellent Coating:

Product: Sure Klean Weather Seal Siloxane PD.

Description: Water based, silane/siloxane water repellent coating.

Solids content: 4 percent.

* + - 1. VOC content: Maximum 30 grams per liter.

\*\*\*\* OR \*\*\*\*

Water Repellent Coating:

Product: Sure Klean Weather Seal Siloxane WB Concentrate.

Description: Water based, solvent-free silane/oligomeric alkoxysiloxane water repellent coating.

Solids content: 48 percent.

* + - 1. VOC content: Maximum 41 grams per liter.

\*\*\*\* OR \*\*\*\*

Water Repellent Coating:

Product: Saltguard.

Description: Solvent based, silane/siloxane water repellent coating and chloride screen.

Solids content: 9 percent.

VOC content: Maximum 713 grams per liter.

\*\*\*\* OR \*\*\*\*

Water Repellent Coating:

Product: Saltguard WB.

Description: Water based, silane/siloxane water repellent coating and chloride screen.

Solids content: 4.2 percent.

VOC content: Maximum 25 grams per liter.

\*\*\*\* OR \*\*\*\*

Water Repellent Coating:

Product: Saltguard VOC.

Description: VOC compliant, silane/siloxane water repellent coating and chloride screen.

Solids content: 9.21 percent.

VOC content: Maximum 100 grams per liter.

\*\*\*\* OR \*\*\*\*

Water Repellent Coating:

Product: Sure Klean Weather Seal Natural Stone Treatment.

Description: Modified siloxane water repellent coating.

Solids content: 9 percent.

VOC content: Maximum 713 grams per liter.

\*\*\*\* OR \*\*\*\*

Water Repellent Coating:

Product: Sure Klean Weather Seal Natural Stone Treatment WB Plus.

Description: Water based modified siloxane water repellent coating.

Solids content: 15 percent.

VOC content: Maximum 100 grams per liter.

\*\*\*\* OR \*\*\*\*

Water Repellent Coating:

Product: Sure Klean Weather Seal Natural Stone Treatment VOC.

Description: Modified siloxane water repellent coating.

Solids content: 9 percent.

VOC content: Maximum 120 grams per liter.

EXECUTION

APPLICATION

Apply in accordance with manufacturer's instructions.

SCHEDULE

Apply coatings to following exterior surfaces:

* + - 1. [Cast-in-place concrete.]
      2. [Precast concrete.]
      3. [Brick unit masonry.]
      4. [Concrete unit masonry.]
      5. [Stone.]
      6. [Cast stone.]
      7. [Brick] [Precast concrete] Stone] pavers.
      8. [\_\_\_\_.]

END OF SECTION