SECTION 09 96 23 – GRAFFITI-RESISTANT COATINGS

 GENERAL

 SUBMITTALS

 Action Submittals:

 Product Data: Manufacturer’s descriptive data and product attributes.

 Closeout Submittals:

 Maintenance Data.

 QUALITY ASSURANCE

 Applicator Qualifications: Firm specializing in work of this Section, with minimum [2] [\_\_] years’ experience.

 Mockup: Minimum [\_\_x \_\_] feet.

 PRODUCTS

 MANUFACTURERS

 Contract Documents are based on products by PROSOCO, Inc. [www.PROSOCO.com](http://www.prosoco.com)

 Substitutions: [Refer to Division 01.] [Not permitted.]

 MATERIALS

 Graffiti Resistant Coating:

 Product: Sure Klean Weather Seal Blok-Guard and Graffiti Control WB 6.

 Description: Clear, breathable, penetrating, water based, single component, silicone elastomer, water and graffiti repellent coating.

 Solids content: 6 percent.

 VOC content: Maximum 20 grams per liter.

 \*\*\*\* OR \*\*\*\*

 Graffiti Resistant Coating:

 Product: Sure Klean Weather Seal Blok-Guard and Graffiti Control WB 15.

 Description: Clear, breathable, penetrating, water based, single component, silicone elastomer, water and graffiti repellent coating.

 Solids content: 15 percent.

 VOC content: Maximum 50 grams per liter.

\*\*\*\* OR \*\*\*\*

 Graffiti Resistant Coating:

 Product: Sure Klean Weather Seal Blok-Guard and Graffiti Control 9.

 Description: Clear, breathable, penetrating, solvent based, single component, silicone elastomer water and graffiti repellent coating.

 Solids content: 9 percent.

 VOC content: Greater than 600 grams per liter.

\*\*\*\* OR \*\*\*\*

 Graffiti Resistant Coating:

 Product: Sure Klean Weather Seal Blok-Guard and Graffiti Control 15.

 Description: Clear, solvent based, single component, silicone elastomer water and graffiti repellent coating.

 Solids content: 15 percent.

 VOC content: Greater than 600 grams per liter.

\*\*\*\* OR \*\*\*\*

 Graffiti Resistant Coating:

 Product: Sure Klean Weather Seal Blok-Guard and Graffiti Control VOC 9.

 Description: Clear, breathable, penetrating, VOC-exempt, solvent based, single component, silicone elastomer water and graffiti repellent coating.

 VOC content: Maximum 100 grams per liter.

 Solids content: 9 percent.

 VOC content: Maximum 100 grams per liter.

\*\*\*\* OR \*\*\*\*

 Graffiti Resistant Coating:

 Product: Sure Klean Weather Seal Blok-Guard and Graffiti Control VOC 15.

 Description: Clear, penetrating, VOC-exempt, solvent based, single component, silicone emulsion water and graffiti repellent coating.

 Solids content: 15 percent.

 VOC content: Maximum 100 grams per liter.

 MATERIALS

 Graffiti Resistant Coating:

 Product: Sure Klean Sacrificial Coating SC-1.

 Description: Clear, water based, sacrificial graffiti resistant coating.

 VOC content: Maximum 30 grams per liter.

 EXECUTION

 APPLICATION

 Apply in accordance with manufacturer's instructions.

 SCHEDULE

 Apply coatings to following above-grade exterior surfaces:

* + - 1. [Cast-in-place concrete.]
			2. [Precast concrete.]
			3. [Brick unit masonry.]
			4. [Concrete unit masonry.]
			5. [Stone.]
			6. [Cast stone.]
			7. [\_\_\_\_.]

END OF SECTION