PROSOCO, Inc. Distributed by ZeroDocs.com

SECTION 09 96 23 – GRAFFITI-RESISTANT COATINGS

GENERAL

SUBMITTALS

Action Submittals:

Product Data: Manufacturer’s descriptive data and product attributes.

Closeout Submittals:

Maintenance Data.

QUALITY ASSURANCE

Applicator Qualifications: Firm specializing in work of this Section, with minimum [2] [\_\_] years’ experience.

Mockup: Minimum [\_\_x \_\_] feet.

PRODUCTS

MANUFACTURERS

Contract Documents are based on products by PROSOCO, Inc. [www.PROSOCO.com](http://www.prosoco.com)

Substitutions: [Refer to Division 01.] [Not permitted.]

MATERIALS

Graffiti Resistant Coating:

Product: Sure Klean Weather Seal Blok-Guard and Graffiti Control WB 6.

Description: Clear, breathable, penetrating, water based, single component, silicone elastomer, water and graffiti repellent coating.

Solids content: 6 percent.

VOC content: Maximum 20 grams per liter.

\*\*\*\* OR \*\*\*\*

Graffiti Resistant Coating:

Product: Sure Klean Weather Seal Blok-Guard and Graffiti Control WB 15.

Description: Clear, breathable, penetrating, water based, single component, silicone elastomer, water and graffiti repellent coating.

Solids content: 15 percent.

VOC content: Maximum 50 grams per liter.

\*\*\*\* OR \*\*\*\*

Graffiti Resistant Coating:

Product: Sure Klean Weather Seal Blok-Guard and Graffiti Control 9.

Description: Clear, breathable, penetrating, solvent based, single component, silicone elastomer water and graffiti repellent coating.

Solids content: 9 percent.

VOC content: Greater than 600 grams per liter.

\*\*\*\* OR \*\*\*\*

Graffiti Resistant Coating:

Product: Sure Klean Weather Seal Blok-Guard and Graffiti Control 15.

Description: Clear, solvent based, single component, silicone elastomer water and graffiti repellent coating.

Solids content: 15 percent.

VOC content: Greater than 600 grams per liter.

\*\*\*\* OR \*\*\*\*

Graffiti Resistant Coating:

Product: Sure Klean Weather Seal Blok-Guard and Graffiti Control VOC 9.

Description: Clear, breathable, penetrating, VOC-exempt, solvent based, single component, silicone elastomer water and graffiti repellent coating.

VOC content: Maximum 100 grams per liter.

Solids content: 9 percent.

VOC content: Maximum 100 grams per liter.

\*\*\*\* OR \*\*\*\*

Graffiti Resistant Coating:

Product: Sure Klean Weather Seal Blok-Guard and Graffiti Control VOC 15.

Description: Clear, penetrating, VOC-exempt, solvent based, single component, silicone emulsion water and graffiti repellent coating.

Solids content: 15 percent.

VOC content: Maximum 100 grams per liter.

MATERIALS

Graffiti Resistant Coating:

Product: Sure Klean Sacrificial Coating SC-1.

Description: Clear, water based, sacrificial graffiti resistant coating.

VOC content: Maximum 30 grams per liter.

EXECUTION

APPLICATION

Apply in accordance with manufacturer's instructions.

SCHEDULE

Apply coatings to following above-grade exterior surfaces:

* + - 1. [Cast-in-place concrete.]
      2. [Precast concrete.]
      3. [Brick unit masonry.]
      4. [Concrete unit masonry.]
      5. [Stone.]
      6. [Cast stone.]
      7. [\_\_\_\_.]

END OF SECTION