Barron Designs Developed by ZeroDocs.com

SECTION 06 61 16 – SIMULATED [STONE] [BRICK] COLUMN COVERS

 GENERAL

 ADMINISTRATIVE REQUIREMENTS

 Pre-Installation Conference:

 Attendance: [Architect,] [Owner,] [Contractor,] [Construction Manager,] [Design/Builder] installer, and related trades.

 Review: Project conditions, manufacturer requirements, delivery and storage, staging and sequencing, and protection of completed work.

 SUBMITTALS

 Action Submittals:

 Product Data: Manufacturer’s descriptive data and product attributes.

 Samples: Verification samples.

 Informational Submittals:

 Certificate of Compliance: Certification that installed products meet specified fire hazard classification.

 QUALITY ASSURANCE

 Installer Qualifications: Minimum [2] [\_\_] years’ experience in work of this Section.

 Fire Hazard Classification: Maximum flame spread/smoke developed rating of 25/450, tested to ASTM E84.

 Mockup: [One] [\_\_\_\_] full size column cover. Approved mockup [may] [may not] remain as part of the Work.

 WARRANTY

 Manufacturer’s standard 15-year warranty for manufacturing defects.

 PRODUCTS

 MANUFACTURERS

 Contract Documents are based on products by Barron Designs, [www.barrondesigns.com](http://www.barrondesigns.com).

 Substitutions: [Refer to Division 01.] [Not permitted.]

 COMPONENTS

 Simulated Stone Column Covers:

 Material: Polyurethane.

 Style: [Colorado Dry Stack Stone, Medium.] [Colorado Dry Stack Split, Narrow.] [Colorado Dry Stack, Medium/Tall.]

 Style: [Windsor Split, Narrow.] [Windsor, Narrow, One Piece.] [Windsor, Medium.]

 Style: [Wellington, Wide.] [Wellington, Medium.]

 Style: [Tumbled Stone, Narrow, One Piece.]

 Style: [Ashford Ledgestone, Wide, One Piece.]

 Style: [Carlton Hampton Cobblestone, Narrow, One Piece.] [Carlton Hampton Cobblestone, Narrow.] [Carlton Hampton Cobblestone, Medium, One Piece.] [Carlton Lehigh Cobblestone, Wide, One Piece.] [Carlton Lehigh Cobblestone, Medium, One Piece.] [Carlton Castle Rock, Medium, One Piece.] [Carlton Castle Rock, Wide, One Piece.]

 Impact resistance: Minimum 60 inch-pounds, tested to ASTM E2486.

 Mold resistance: 10, tested to ASTM D3273.

 Color: [\_\_\_\_.]

 Accessories:

* + - * 1. Caps: [Colorado Dry Stack 6 Inch Split Post Cap, Medium.] [Colorado Dry Stack 6 Inch Split Post Cap, Narrow.] [Colorado Dry Stack 4 Inch Split Post Cap, Narrow.] [Colorado Dry Stack Solid, Medium.] [Colorado Dry Stack Solid, Narrow.]
				2. Caps: Tumbled Stone.
				3. Caps: [Windsor Column Cap, Narrow.] [Windsor Column Cap, Medium.]
				4. Caps: [Carlton Peaked, Medium.] [Carlton Live Edge.] [Carlton Flat, Medium.] [Carlton Crown, Wide.] [Carlton Crown, Narrow.] [Carlton Live Edge, Narrow.] [Carlton Pyramid, Narrow.] [Carlton Pyramid, Wide.]
				5. Caps: [Ashford Ledgestone, Flat, Wide.] [Ashford Ledgestone, Wide.] [Ashford Pyramid, Wide.]
				6. Caps: [Wellington, Wide.] [Wellington, Medium.]
				7. Stack sections: Ashford Ledgestone, Wide.
				8. Risers: Tumbled Stone.
				9. Pedestals: [Carlton Base, Narrow.] [Carlton Base, Wide.] [Carlton Base, Wide and Tall.]

 Simulated Brick Column Covers:

 Material: Polyurethane.

 Style: [Carlton Traditional Brick, Narrow, One Piece.] [Carlton Traditional Brick, Medium, One Piece.] [Carlton Traditional Brick, Wide, One Piece.]

 Impact resistance: Minimum 60 inch-pounds, tested to ASTM E2486.

 Mold resistance: 10, tested to ASTM D3273.

 Color: [\_\_\_\_.]

 ACCESSORIES

 Adhesive and Fasteners: Types recommended by column cover manufacturer.

 Joint Sealer: Textured, color matched to column cover, type recommended by column cover manufacturer.

 EXECUTION

 INSTALLATION

 Install in accordance with manufacturer’s instructions.

END OF SECTION