SECTION 09 65 19 – RESILIENT TILE FLOORING

GENERAL

SUBMITTALS

Action Submittals:

Product Data: Manufacturer’s descriptive data and product attributes for flooring.

Samples: [Selection samples.] [Verification samples.]

Informational Submittals:

Certificate of Compliance: Certification that installed products meet specified fire hazard and coefficient of friction requirements.

Closeout Submittals:

Extra materials: [One unopened carton] [[\_\_] unopened cartons] [[\_\_] percent] [[\_\_] square feet] of each tile.

QUALITY ASSURANCE

Installer Qualifications: Firm specializing in work of this Section with minimum [2] [\_\_] years’ experience.

Regulatory Requirements:

Dynamic coefficient of friction: Minimum [0.43,] [\_\_,] tested to ANSI A326.3.

Fire hazard classification: Class [I] [\_\_] rated, tested to ASTM E648.

Mockup: [8 x 8] [\_\_ x \_\_] feet. Approved mockup [may] [may not] remain as part of the Work.

PRODUCTS

MANUFACTURERS

Contract Documents are based on products by Wego International Floors. [www.wegointernationalfloors.com](http://www.wegointernationalfloors.com/)

Substitutions: [Refer to Division 01.] [Not permitted.]

MATERIALS

Luxury Vinyl Tile:

Product: Sound Pro.

Composition: 0.5 mm wear layer, 0.7 mm vinyl, 1.0 mm pad, 4.5 mm SPC core, and 1.5 mm EVA attached pad.

Static Load Resistance: 0.10mm, ASTM F970.

Residual Indentation: 0.177mm, ASTM F1914.

Coefficient of Friction: 0.51 Dry, 0.49 wet, ASTM D2047.

Overall thickness: 8.2 mm.

Size: 9 inches wide x 60 inches long.

Surface texture: Embossed.

Finish: UV urethane.

Edges: Four-sided micro bevel.

Installation method: Floating; Unilin click system.

Color: [\_\_\_\_.] [To be selected from manufacturer’s full color range.]

EXECUTION

INSTALLATION

Install in accordance with manufacturer's instructions.

Installation Method: Floating.

END OF SECTION