SECTION 09 65 19 – RESILIENT TILE FLOORING

 GENERAL

 SUBMITTALS

 Action Submittals:

 Product Data: Manufacturer’s descriptive data and product attributes for flooring.

 Samples: [Selection samples.] [Verification samples.]

 Informational Submittals:

 Certificate of Compliance: Certification that installed products meet specified fire hazard and coefficient of friction requirements.

 Closeout Submittals:

 Extra materials: [One unopened carton] [[\_\_] unopened cartons] [[\_\_] percent] [[\_\_] square feet] of each tile.

 QUALITY ASSURANCE

 Installer Qualifications: Firm specializing in work of this Section with minimum [2] [\_\_] years’ experience.

 Regulatory Requirements:

 Dynamic coefficient of friction: Minimum [0.43,] [\_\_,] tested to ANSI A326.3.

 Fire hazard classification: Class [I] [\_\_] rated, tested to ASTM E648.

 Mockup: [8 x 8] [\_\_ x \_\_] feet. Approved mockup [may] [may not] remain as part of the Work.

 PRODUCTS

 MANUFACTURERS

 Contract Documents are based on products by Wego International Floors. [www.wegointernationalfloors.com](http://www.wegointernationalfloors.com/)

 Substitutions: [Refer to Division 01.] [Not permitted.]

 MATERIALS

 Luxury Vinyl Tile:

 Product: Sound Pro.

 Composition: 0.5 mm wear layer, 0.7 mm vinyl, 1.0 mm pad, 4.5 mm SPC core, and 1.5 mm EVA attached pad.

 Static Load Resistance: 0.10mm, ASTM F970.

 Residual Indentation: 0.177mm, ASTM F1914.

 Coefficient of Friction: 0.51 Dry, 0.49 wet, ASTM D2047.

 Overall thickness: 8.2 mm.

 Size: 9 inches wide x 60 inches long.

 Surface texture: Embossed.

 Finish: UV urethane.

 Edges: Four-sided micro bevel.

 Installation method: Floating; Unilin click system.

 Color: [\_\_\_\_.] [To be selected from manufacturer’s full color range.]

 EXECUTION

 INSTALLATION

 Install in accordance with manufacturer's instructions.

 Installation Method: Floating.

END OF SECTION