EPRO Services, Inc. Developed by ZeroDocs.com

 08//20202

This section includes editing notes to assist the user in editing the section to suit project requirements. These notes are included as hidden text, and can be revealed or hidden by the following method in Microsoft Word:

 Display the FILE tab on the ribbon, click OPTIONS, then DISPLAY. Select of deselect HIDDEN TEXT.

This guide specification section has been prepared by EPRO Services, Inc. for use in the preparation of a project specification section covering PreTak Pre-Adhered Blindside Waterproofing for use on below-grade walls and under concrete slabs.

The following should be noted in using this specification:

Hypertext links to manufacturer websites are included after manufacturer names to assist in product selection and further research. Hypertext links are contained in blue, e.g.:

www.zerodocs.com

Optional text requiring a selection by the user is enclosed within brackets and as red text, e.g.: Color: [Red.] [Black.]"

Items requiring user input are enclosed within brackets and as red text, e.g.: "Section [\_\_ \_\_ \_\_ - \_\_\_\_\_\_\_\_]."

Optional paragraphs are separated by an "OR" statement included as red text, e.g.:

 \*\*\*\* OR \*\*\*\*

For assistance in the use of products in this section, contact EPRO Services, Inc. by calling 800-882-1896 or visit their website at [www.eproinc.com](http://www.eproinc.com).

This specification has been prepared based on SimpleSpecs specification templates. The SimpleSpecs Master Guide Specification system comprises a full architectural master specification that can be used to specify all project requirements. For additional information on SimpleSpecs products visit the ZeroDocs.com website at www.zerodocs.com.

**SECTION 07 13 56 – BLINDSIDE WATERPROOFING**

1. **GENERAL**
	1. ADMINISTRATIVE REQUIREMENTS
		1. Pre-Installation Conference:
			1. Attendance: [Architect,] [Owner,] [Contractor,] [Construction Manager,] installer, and related trades.
			2. Review: Project conditions, manufacturer requirements, delivery and storage, staging and sequencing, and protection of completed work.
	2. SUBMITTALS

* + 1. Action Submittals:
			1. Shop Drawings: Illustrate products, installation, and relationship to adjacent construction.
			2. Product Data: Manufacturer’s descriptive data and product attributes.
		2. Informational Submittals:
			1. Certificate of Compliance: Certification that installed products meet specified design and performance requirements.
	1. QUALITY ASSURANCE
		1. Installer Qualifications: Firm specializing in work of this Section, with minimum [2] [\_\_] years’ experience.
	2. WARRANTY
		1. Manufacturer’s 1 year warranty against defective materials.
1. **PRODUCTS**
	1. MANUFACTURERS
		1. Contract Documents are based on PreTak by EPRO Services, Inc. [www.eproinc.com](http://www.eproinc.com)
		2. Substitutions: Refer to Division 01.
	2. MATERIALS
		1. Blindside Waterproofing Sheet:
			1. Product: PreTak.
			2. Description: 46 mil thick fully adhered waterproofing sheet membrane comprised of long fiber HDPE film coated with PSA gel and protected by plastic release liner.
			3. Edges: [Pre-treated adhesive selvage edge.] [adhesive selvage edge.]
			4. Properties:
				1. Film tensile strength: 4742 PSI, tested to ASTM D412.
				2. Elongation: 722 percent, tested to ASTM D412.
				3. Resistance to water vapor transmission: 0.087 perms, tested to ASTM E96, Method B.
				4. Resistance to hydrostatic water pressure: 715 feet, tested to ASTM D751.
				5. Methane permeability: Pass ASTM D1434.
2. **EXECUTION**
	1. INSTALLATION
		1. Install in accordance with manufacturer’s instructions and approved Shop Drawings.

 END OF SECTION