Hydro-Blok Distributed by ZeroDocs.com

SECTION 09 28 23 – TILE BACKING BOARDS

 GENERAL

 SUBMITTALS

 Action Submittals:

 Product Data: Manufacturer’s descriptive data and product attributes.

 QUALITY ASSURANCE

 Installer Qualifications: Firm specializing in work of this Section, with minimum [2] [\_\_] years’ experience.

 PRODUCTS

 MANUFACTURERS

 Contract Documents are based on products by Hydro-Blok (844) 588-9559, [www.hydroblok.com](http://www.hydroblok.com)

 Substitutions: [Refer to Division 01.] [Not permitted.]

 MATERIALS

 Tile Backing Boards:

 Product: Hydro-Block Wall and Building Board.

 Description: Prefabricated sloped shower pan.

 Composition: Waterproof extruded polystyrene core faced both sides with woven mesh and cementitious coating.

 Density: 2.0 PCF.

 Compressive Strength: Minimum 36psi, when tested to ASTM D1621.

 R-Value: 2.2 per 1/2-inch thickness.

 Meet IAPMO PS 106.

 Size: [36 x 60 inches x 1/4 inch] [36 x 60 inches x 1/2 inch] [48 x 64 inches x 1/2 inch] [48 x 96 x 1/2 inch] [36 x 60 inches x 5/8 inch] [36 x 60 inches x 1.0 inch] [25 x 48 inches x 1.5 inch] [36 x 48 inches x 1.5 inch] [48 x 60 inches x 2.0 inch]

 ACCESSORIES

 Fasteners: ASTM C1513 screws, hot-dip galvanized or fluoropolymer coated steel.

 EXECUTION

 INSTALLATION

 Install in accordance with manufacturer's instructions.

 Fasten panels to framing at maximum [12] [16] [\_\_] inches on center.

END OF SECTION