Hydro-Blok Distributed by ZeroDocs.com

SECTION 09 28 23 – TILE BACKING BOARDS

GENERAL

SUBMITTALS

Action Submittals:

Product Data: Manufacturer’s descriptive data and product attributes.

QUALITY ASSURANCE

Installer Qualifications: Firm specializing in work of this Section, with minimum [2] [\_\_] years’ experience.

PRODUCTS

MANUFACTURERS

Contract Documents are based on products by Hydro-Blok (844) 588-9559, [www.hydroblok.com](http://www.hydroblok.com)

Substitutions: [Refer to Division 01.] [Not permitted.]

MATERIALS

Tile Backing Boards:

Product: Hydro-Block Wall and Building Board.

Description: Prefabricated sloped shower pan.

Composition: Waterproof extruded polystyrene core faced both sides with woven mesh and cementitious coating.

Density: 2.0 PCF.

Compressive Strength: Minimum 36psi, when tested to ASTM D1621.

R-Value: 2.2 per 1/2-inch thickness.

Meet IAPMO PS 106.

Size: [36 x 60 inches x 1/4 inch] [36 x 60 inches x 1/2 inch] [48 x 64 inches x 1/2 inch] [48 x 96 x 1/2 inch] [36 x 60 inches x 5/8 inch] [36 x 60 inches x 1.0 inch] [25 x 48 inches x 1.5 inch] [36 x 48 inches x 1.5 inch] [48 x 60 inches x 2.0 inch]

ACCESSORIES

Fasteners: ASTM C1513 screws, hot-dip galvanized or fluoropolymer coated steel.

EXECUTION

INSTALLATION

Install in accordance with manufacturer's instructions.

Fasten panels to framing at maximum [12] [16] [\_\_] inches on center.

END OF SECTION