M-D PRO		Distributed by ZeroDocs.com

SECTION 09 30 43 – TILING ACCESSORIES

GENERAL

SUBMITTALS

Action Submittals:

Product Data: Manufacturer’s descriptive data and product attributes.

QUALITY ASSURANCE

Installer Qualifications: Firm specializing in work of this Section, with minimum [2] [__] years’ experience.

PRODUCTS

MANUFACTURERS

Contract Documents are based on products by M-D PRO, www.mdpro.com/prova

Substitutions: [Refer to Division 01.] [Not permitted.]

MATERIALS

Tile Underlayment:

Product: Prova-Flex.

Description: Lightweight uncoupling membrane.

Comply with ANSI A118.12.

Rating: Extra Heavy Performance Rating, tested to ASTM C627.

Thickness: 0.16” (4 mm).

**** OR ****

Tile Underlayment:

Product: Prova Flex-Heat.

Description: Lightweight uncoupling membrane with heating cable capabilities.

Comply with ANSI A118.12.

Rating: Extra Heavy Performance Rating, tested to ASTM C627.

Thickness: 0.26” (6.5 mm).

**** OR ****

Tile Underlayment:

Product: Protegga Plus.

Description: Lightweight uncoupling membrane.

Comply with ANSI A118.12.

Rating: Extra Heavy Performance Rating, tested to ASTM C627.

Thickness: 0.16” (4 mm).

Shower Pan:

Product: Prova Pan.

Description: Prefabricated sloped shower pan.

Density: 2.75 lb./ft.3 (44.05 kg/m3).

Size and drain location: [48” x 48” (122 cm x 122 cm), center drain.] [32” x 60” (81 cm x 152 cm), offset drain.] [32” x 60” (81 cm x 152 cm), center drain.]

Accessories: Prova Pan Extension, as required to suit project conditions.

Shower Pan:

Product: Prova Pan-Multi.

Description: Prefabricated sloped shower pan.

Density: 3.5 lb./ft.3 (56.06 kg/m3).

Size: 60” x 60” x 7/8” thick (152 cm x 152 cm x 2.2 cm thick).

Drain location: Center.

Extensions: Prova Pan-Multi Extension, as required to suit project conditions.

**** OR ****

Shower Pan:

Product: Prova Linear Pan.

Description: Prefabricated linear sloped shower pan.

Density: 2.75 lb./ft.3 (44.05 kg/m3).

Size: 22.5” x 24” x 1-5/8” thick (57 cm x 61 cm x 4.1 cm thick).

Accessories: Provide as required to suit project conditions.

Prova Linear Pan Extension.

Side supports.

Filler strips.

Shower Waterproofing:

Product:  Prova-Mat.

Description: Low-perm waterproofing membrane.

Comply with ANSI A118.10.

Water vapor transmission: Maximum 0.115 perms, tested to ASTM E96/E96M.

Thickness: 0.43 mm.

Accessories:

Joint sealing strip: Prova Joint.

Prefabricated corners: ProvaCorner.

Pipe seal: Prova Pipe Seal.

Shower Drains:

Product:  Prova Drain.

Description: Coated [ABS] [PVC] drain body with [stainless steel] [chrome] [brass] bronze] graphite] [black] drain cover.

Meet ASME A112.18.2-2020/CSA B125.2-20.

Linear Drains:

Product:  Prova Linear Drain.

Description: Coated drain body with waterproofing membrane adhered to drain flange.

Meet ASME A112.18.2-2020/CSA B125.2-20.

Width: [24” (61 cm)] [36” (91 cm)] [42” (107 cm)].

Drain grate: Prova Linear Grate.

Prefabricated Niches:

Product: Prova Niche.

Description: Prefabricated tile backing board.

Meet IAPMO PS 106.

Inside dimensions: [16” x 16” (40.6 cm x 40.6 cm)] [24” x 16” (61 cm x 40.6 cm)] [33” x 16” (83.8 cm x 40.6 cm)].

Shelves: [None.] [3/8” (9.5 mm) thick clear laminated glass shelves, [one] [two] per niche.]

Prefabricated Shower Curbs:

Product: Prova Curb.

Description: Prefabricated expanded polystyrene low-profile shower curb.

Density: 3.0 PCF.

Size: 4-1/2” (11 cm) x 4” (10 cm) x [48” (122 cm)] [60” (152 cm)] long.

Tile Edgings:

Product: Prova Tile Edge.

Material: Aluminum.

Color and finish: [Mill finish.] [Anodized, [brushed] [bright] finish, [____] color [to be selected from manufacturer’s full color range.] [Powder coated, [____] color [to be selected from manufacturer’s full color range.]

Profiles:

Flat Tile Edge.

Round Tile Edge.

Round Outside Corner.

Round Inside Corner.

Square Tile Edge.

Square Corner.

Ceramic Cove.

Ceramic Cove Corner.

J-Molding.

Ceramic Adapter.

Ceramic Reducer.

Ceramic Tile Stair Nosing.

Decorative Tile Stair Nosing.

Dual-Purpose Decorative Edging.

Counter Top/Stair Nosing.

Counter Top Corner.

T-Molding.

T-Molding Reducer.

Anti-Skid Stair nosing with vinyl insert.

Ceramic Edge Protection Ramp.

Heavy-Duty Expansion Joint with vinyl insert.

**** OR ***

Tile Edgings:

Material: Stainless steel.

Profiles:

Flat Tile Edge.

Round Tile Edge.

Round corner.

Square Tile Edge.

Square Corner.

**** OR ****

Tile Edgings:

Material: PVC.

Profiles:

Vinyl Tile Edge.

Vinyl J-Cap.

Heavy Duty Vinyl Edge – Flat.

Heavy Duty Vinyl Edge – Round.

Round Corner.

Expansion Joint.

EXECUTION

INSTALLATION

Install in accordance with manufacturer's instructions.

END OF SECTION